Supplemental Information for
Photochemical CVD of Ru on Functionalized Self-Assembled Monolayers from Organometallic Precursors
Kelsea R. Johnsona, Paul Arevalo Rodriguezb, Christopher R. Brewera, Joseph A. Brannakaa, Zhiwei Shib, Jing Yangb, Bryan Salazarc, Lisa McElwee-White,a, [1] Amy V. Walkerb,c,1
[1] Corresponding Author: (LMW) Email: lmwhite@chem.ufl.edu, Ph: 352 392 8768, Fax: 352 846 0296; (AVW) Email: amy.walker@utdallas.edu, Ph: 972 883 5780, Fax: 972 883 5725
aDepartment of Chemistry, University of Florida, Gainesville, FL 32611-7200, USA
bDepartment of Materials Science and Engineering, University of Texas at Dallas, 800 W. Campbell Rd, Richardson, TX 75080, USA
cDepartment of Chemistry and Biochemistry, University of Texas at Dallas, Richardson, Texas 75080, USA

Figure S1. High resolution positive ion mass spectra centered at m/z 102 before and after exposure to CpRu(CO)2Me on (a) –COOH and (b) –OH terminated SAMs. After deposition some of the samples were rinsed in hexane (“rinse”). Deposition conditions: 6000 L CpRu(CO)2Me, deposition time 5 mins, pressure 2 x 10-5 torr and 500 W Hg arc lamp.

Figure S2. Photoelectron spectra of Ru 3p3/2 after exposure to (a) 6000 L (η3-allyl)Ru(CO)3Br and (b) 6000 L CpRu(CO)2Me on –COOH terminated SAMs. Deposition conditions: deposition time 5 min, pressure 2 x 10-5 torr and 500 W Hg arc lamp.

The Ru 3p3/2 binding energy has been reported to be 461.2–462.2 eV in Ru, 462.4-463.2 in RuO2, 464.3-465.0 eV in RuOx/Ru and 461.8-461.9 eV in Ru/RuOx.1,2 The data therefore confirm that Ru likely remains in the +2 oxidation state. We note that the Ru 2p1/2 peak is also observed (with a spin-orbit splitting of ~22 eV in agreement with previous studies3) but is low intensity and thus noisy, and so we were unable to obtain a precise position of the peak to further confirm the assignment of the Ru species.

References
1	NIST X-ray Photoelectron Spectroscopy Database, Version 4.1 (National Institute of Standards and Technology, Gaithersburg, 2012).
2	J. Y. Shen, A. Adnot, and S. Kaliaguine, Appl. Surf. Sci. 51, 47-60 (1991).
3	A. J. Mc Evoy and W. Gissler, phys. stat. sol. (a) 69, K91-K96 (1982).